Cytotoxicity and Inflammatory Effect of Silver Nanoparticles

in Human Cells

Cytotoxicity and Inflammatory Effect

of Silver Nanoparticles

in Human Cells

Jeong-shin Park, Na Mi Yu, Jinwoo Cheon and In-Hong Choi

Department of Microbiology, College of Medicine;

Department of Chemistry;

Nanomedical NCRC, Yonsei University, Seoul, Korea

1. Approaches to practical toxicology tests

to assess nanoparticles

2. Cytotoxicity and inflammatory effects

of silver nanoparticles

Nanoparticles and toxicity assay

The rapidly developing field of nanotechnology will result

in exposure of nanoparticles to humans via several routes

(e.g., inhalation, ingestion, skin, etc.). Nanoparticles can

translocate from the route of exposure to other vital

organs and penetrate cells.

• Toxicity studies to determine the deleterious effects of

nanoparticles on living cells are required.

• Due to the nanosize and the nature of agglomeration,

simple standard methods to characterize the biological

effects of nanoparticles are currently unavailable.

• In this study, practical information regarding the optimal in

vitro tests for nanotoxicity were evaluated.

Silver nanoparticles

03/19

Antimicrobial applications

Ink

Cosmetics 200nm 200nm 500nm

20 nm (synthetic)

180 nm

(commercial,

Aldrich)

| Biological tests Inflammation (( Annexin staining,caspase activation ((Cytokine production,activation of Signaling molecule ((ROS ((Cytotoxicity(( MTT/CCK-8 (( Establishment of in vitro toxicity assay (( Identification of mechanisms for toxicity and inflammation | Synthesis Production & characterization of physical and chemical properties |
| --- | --- |

In vitro tests for nanoparticles

| ISO/TC229 • OECD • U.S NCL Review in vitro methods | • Production of diverse particles (size, surface) • Assess biological activities Assess toxicity tests | Understanding of proper methods for nanoparticles Establish proper methods |
| --- | --- | --- |

Exposure routes of nanomaterials

Skin      Respiratory trac   Immune System

|  | Cell line | Origin | Characteristics |  |
| --- | --- | --- | --- | --- |
| Respiratory | A549 | Lung epithelial | Proper for cytotoxicity |  |
|  | BEAS-2B | Bronchial epithelial |  |  |
|  |  |  | Proper for cytokine Production |  |
| Immune | U937 | Macrophage | Proper for cytotoxicity and cytokine production |  |
| Skin | SK-Mel | Skin epithelial | Proper for cytotoxicity and cytokine production |  |
|  | A375 | Skin epithelial | Too fast growing |  |

Standard toxicology tests and silver nanoparticles

| In Vitro Immunology Properties (Blood contact | Hemolysis | Release of hemoglobin | Standard | Proper |
| --- | --- | --- | --- | --- |
|  | Complement activation |  |  |  |
|  |  | Activation of C3 complement | Standard | Inappropriate |
|  |  | Leukocyte proliferation with mitogen stimulation | Standard | CCK-8 |
| In Vitro Immunology (Cell-based assays) | Leukocyte proliferation | Zymosan assay | Standard | Proper |
|  |  | Cytokine production | Standard | Proper |
|  | Phagocytosis |  |  | Proper |
|  | Cytokine induction |  |  |  |
| Toxicity | Oxidative stress | Detection of ROS | Standard | CCK-8 |
|  | Cytotoxicity (necrosis) | Cell viability and mitochondrial integrity | Standard | Annexin-V |
|  | Cytotoxicity (apoptosis) |  |  |  |
|  |  | Activation of caspase 3 | Standard |  |
| Targeting | Cell binding/internalization | N/S | N/S | TEM, confocal microscope or other methods |

Characteristics specific to metal nanomaterials

Nanoparticles larger than 100 nm tend to aggregate relatively quickly in vitro when compared to nanoparticles smaller than 100 nm. Fresh samples

within two weeks after synthesis is recommended for tests.

•

Each standard toxicology method must be verified before use. (ex. interference with a specific wavelength, electrophoresis)

Flow chart for nanotoxicity tests

Small –Nano Particle Size 100nm-Large

Small--Analysis Of Biological --- Nano Particle Size 100nm

- Particle size

- Cytotoxicityroperties

- Apoptosis

- Cytokine production

- Hemolysis

- Leukocyte proliferation

- ROS production

Large— Analysis of chemical/physical

properties

- Aggregation

- Particle size

Cytotoxicity of silver nanoparticles

20 nm

Cell viability (%)

Conc. (μg/mL)

Cell viability (%)

Conc. (μg/mL)

SK-Mel28 (skin) A375 (skin) A549 (lung)

Summary

In human cells, epithelial cells from skin or lung, and macrophages, 5 nm and 20 nm silver particles induced stronger cytotoxicity and ROS synthesis than 80 nm

particles did.

• 5 nm and 20 nm silver particles induced chemokine  production, mainly IL-8, MIF and RANTES, while proinflammatory cytokines, IL-1, IL-6 and TNF-α were not induced significantly in the same conditions.

• Some MAP kinase signaling pathways were activated during exposure to silver nanoparticles at lower ---concentrations which do not induce cytotoxicity

The toxicity and inflammatory effects of nanoparticles are dependent on their size. In silver nanoparticles smaller than 20 nm induce cytotoxicity significantly in vitro.

• Nanoparticles induce inflammatory immune responses at lower concentrations and chemokines are the major cytokines induced at early stages of exposure to silver